The following table shows heavy metal content of dust samples, taken at the site of a shredding plant.

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| **Parameter** | **As** | **Pb** | **Cd** | **Cr** | **Cu** | **Ni** | **Zn** |
| **Sample** | **[mg/kg dm]** | | | | | | |
| Roads | 17 | 1,30 | 22 | 730 | 7,0 | 600 | 10,1 |
| Dust at shredder | 24 | 3,10 | 85 | 530 | 2,8 | 810 | 21,0 |
| Storage places | 26 | 1,20 | 11 | 1,20 | 3,4 | 790 | 9,50 |